## Slide 1: Typical structure of a digital chip
Pad Frame
I/O circuits
Core (o internal) logic

## Slide 2: Latch-up layout rules: core logic
Every part of a p-active area in an n-well must "see" at least one well-tap with a maximum distance R
Every part of an n-active area in the substrate (p-well) must "see" at least one substrate-tap with a maximum distance R

## Slide 3: I/O circuits: over-voltage risk
possible load / transmission
line equivalent circuit
I/O pad
Vdd
gnd
Vout
Ideal case
Real case
In I/O circuits, the output termination can exceed the Vdd or
gnd rails. This introduces additional risk of latch-up

## Slide 4: Injection of minority carriers
Well: bases of the pnp BJT (collector of npn BJT)
Substrate: bases of the npn BJT (collector of pnp BJT)
when Vout exceeds Vdd,
this diode is turned on
when Vout drops below gnd,
this diode is turned on

## Slide 5: Injection of minority carriers
Hole injection into the n-well
when Vout > Vdd
Electron injection into the substrate when Vout< 0
Injection of minority charge carriers into the parasitic BJTs bases may trigger the latch-up phenomenon

## Slide 6: I/O devices: Guard Rings
n+ (well tap)
p+ (sub. tap)
n-well
p+ (sub-tap)
vdd
gnd
vdd
gnd
gnd
vdd
I/O devices
n-well
p+ (sub. tap)
Guard rings are placed around the I/O devices in order to:
Reduce the resistance between drain/body diffusions to gnd (nMOS) or Vdd (pMOS)
Collect most of the minority carriers injected by one device before they reach neighboring devices
These guard rings further reduce the
effects of the I/O devices on the core
logic
I/O circuits require additional protection against latch-up