## Slide 1: Process Errors in Integrated Circuits
chip
component
(e.g. resistor, transistor, …)
quantity A (e.g.
resistance, bn, Vt etc)
AN (nominal value)
Design phase
Production phase
Dn= number of samples whose value (A) falls in the bin
n= total number of samples

## Slide 2: Components of the error and statistical representation
AN: nominal value
Ai: A for a generic i-th component.
<A>: the mean of the distribution.
eS: Systematic error = <A>-AN
eR: Random error for the i-th component eR =Ai-<A>.
Random error: standard deviation
sA

## Slide 3: Confidence intervals
Max deviation from the mean | ± s | ± 2s | ± 3s | ± 4s
Fraction of data within the interval | 68.3 % | 95.4 % | 99.7 % | 99.994 %
Fraction of data outside the interval | 31.7 % | 4.6 % | 0.3 % | 0.006 %

## Slide 4: Errors in Integrated Circuits: Levels
chip level
wafer level
batch level
run level

## Slide 5: Local and global errors: means
i-th chip
nominally identical components
<A>chip
<A>process
varies from chip to chip (local mean)
property of the whole
process
(global mean)

## Slide 6: Local and global errors
process corners
"max"
process corners
"min"
process corners
"typical"
Random errors local and global
In practice, the distribution of local errors is much narrower than shown here
Chip
Process

## Slide 7: Matching errors: definition
Component 1
Component 2
A1
A2
Nominally
identical and
placed on the
same chip
Random Matching errors: Main causes
Microscopic irregularities (local granularity)
Parameter gradients
Matching error (or mismatch)

## Slide 8: Relationship between matching error and local error
<A>chip
e1
e2
A2
A1
DA

## Slide 9: Matching errors: Microscopic irregularities
N= number of dopants
atoms within the
component area
DN= N1-N2
Depending on the position
DN is subjected to large
variations.
The important parameter is:
Relative matching error:
matching error

## Slide 10: Matching errors: Microscopic irregularities
The number of dopants atoms affects several properties such as effective sheet resistance and MOSFET threshold voltage
The example can be replicated for other quantities, such as oxide thickness, where the crosses in the figure may represent local maxima or minima
The large fluctuation of DN/N can be ascribed to the small area of the devices shown in the example. For even smaller devices its is likely that one of the two devices does not include any dopant atom : DN/N may exceed unity (100 % error).

## Slide 11: Microscopic irregularities: effect of device area
Larger device areas result in smaller relative matching errors

## Slide 12: Microscopic irregularities: the Pelgrom model
Mosfet
Resistor
From: Pelgrom et a IEEE J. of Solid State Circuits, 1989l
Cvt, Cb and CR are constant parameters of the process Their values are given in the Design Rule Manual, with names that depend on the foundry (there is no general convention).
Cvt units are generally V·mm, while Cb and CR ones are mm.

## Slide 13: Matching Errors: Gradients
Gradients indicate that important quantities that affect the device properties are not uniformly distributed on a macroscopic scale. This means that these quantities gradually varies across the chip area.
Quantities of interest can be, for example: -) Dopant density -) Oxide thickness
-) Geometrical process biases (e.g. etching undercut) -) Temperature (e.g. due to power devices present on the chip)
-) Mechanical stress (mainly due to the packaging process)

## Slide 14: Effect of gradients on device matching
In this example radient causes matching error
For this case, gradient does not cause matching error
We consider a generic quantity "A"
Unfortunately, in most cases, the direction of gradients is not predictable!

## Slide 15: Layout rules that prevent device mismatch caused by gradients
Rule 1 (obvious): Take the distance between objects as close as possible. (This rule is less effective for large devices)
Rule 2: Use common centroid configurations.
Centroid of both A1 and A2 objects
A1
A2
A1,1
A1,2
A2,1
A2,2

## Slide 16: Common centroid configuration: Oblique gradients
A1
A2
A1,1
A1,2
A2,1
A2,2
average
average
high
low
component
part
level
The common centroid configuration is effective also against oblique gradients..

## Slide 17: Split and connect components in common centroid configurations
Series are preferred
when resistors R1 and R2
are large
Parallels have to be preferred
for small resistances
Case 1::Resistors

## Slide 18
Split and connect components in common centroid configurations
Other devices -Properties of series and parallels
Accurate: Can be used in common centroid configurations
Not accurate
Don't use!
not allowed in
standard
n-well CMOS

## Slide 19
Split and connect components in common centroid configurations
Case 2: MOSFETS
Capacitors: Parallel connections are preferred (no floating nodes)
Floating node (no dc path)
Series connections of capacitors have to be avoided as much as possible unless dc paths are provided for the floating node
BJTs: Same as Mosfets (parallels only)

## Slide 20: Other Layout rules for improving device matching
Wrong solutions
Different size: poor matching
Different orientation:
poor matching
resistors
mosfets
mechanical stress

## Slide 21: Other Layout rules for improving device matching
Same direction
(to match thermoelectric effects)
Same surroundings
Temperature gradients develop extra voltage differences that depend on the current direction
(up to several hundred mVs

## Slide 22: Summary of rules for a good device matching
Devices must be nominally identical (same dimensions, same orientation)
Device areas should be as large as possible (Pelgrom model)
Place devices as close as possible
Use common centroid configurations
Same current direction for the two devices
The devices should "see" the same surroundings

## Slide 23: Rules to obtain accurate ratios
Example: accurate inverting amplifier with gain magnitude =3
(e.g. with x=0.1, er=11%)
(systematic error)

## Slide 24: Accurate ratios: modular components
Generalization to
Fractional ratios
Both R1 and R2 are obtained by adding different numbers of a single module RN.
module
R1 includes also contact resistances 2RC
R2 is now exactly 3 R1, independently from contact resistances and other non idealities of R1

## Slide 25
Accurate ratios: modular components
Large ratios with less components
Parallel / series
combination
Current mirror with accurate gain
MM = Module

## Slide 26: Elements of error propagation theory
Independent quantity
Dependent quantity
Am is an arbitrary value between A1 and A2

## Slide 27: For multiple independent variables - general case
G1
G2
(A1,B1,C1)
(A2,B2,C2)

## Slide 28: Error propagation: particular case 1
Using:
a,b,g : real exponents
A,B,C real positive variables
posynomial expression
case 1:

## Slide 29: Error propagation: particular case 1
Relative variation (or relative error)
Sum of the single relative errors, weighted by the respective exponents
case 1

## Slide 30: Error propagation: particular case 2
Here we have the absolute error of G, not the relative one.
case 2: logarithm of a posinomial

## Slide 31: Application to matching errors
Generally, when dealing with matching errors: (mean value)
Matching errors has also the following basic property: Linearity: G=A+B DG=DA+DB G=kA, where k is a constant : DG=kDA
In the case of relative error, if G=kA:

## Slide 32: Matching errors: statistical independence
Matching errors of different quantities (e.g., quantities A,B,C) can be often considered independent from each other since they are mostly affected by microscopic irregularities, that do not show significant correlations when pairs of quantities are considered.
In addition matching errors of different device pairs can be also considered independent, or, at least, uncorrelated.