## Slide 1: Back to the sensor types
Wide linearity range, inexpensive, highly integrable.
Hall sensors:
Advantages:
Drawbacks:
Relatively large detection limit (not suitable for B < 1mT)
Magnetic sensors for low and ultra-low magnetic fields:
Anisotropic Magneto-Resistance (AMR sensors)
Giant Magneto-Resistance (GMR) - Tunnel Magneto Resistance (TMR)
Flux Gates

## Slide 2: Anisotropic Magneto Resistance
A premise on magnetization: ferromagnetic materials
IM
IM
N=number of turns
H, B
H: Excitation, proportional to NIM
B: Response to the excitation B=m0(H+M)
M: Due to the material.
In ferromagnetic materials M>>H
Hysteresis
Hard ferromagnetic
Soft ferromagnetic
(idealized)
H and M has different scales in these figures
Coil with a solid core

## Slide 3: Anisotropic ferromagnetic materials
Easy axis
Sensitive axis
Materials that present this characteristic are, for example Iron-Nickel (NixFey) alloys, properly deposited under a magnetic field
The film shape (L >> W ) enhance the anysotropy
Magnetic material (film)
L
W

## Slide 4: Anisotropic Magneto Resistance (AMR)
Material:
Ferromagnetic conductors such as
Fe / Ni alloys (Permalloy)
Discovered: 1856 (Lord Kelvin)
V
BM: permanent magnetization (saturated)
I
Easy axis
Sensitive axis
HE
BE: proportional to the external field to be measured ( HE )

## Slide 5: Resistance vs external magnetic field
q
0
90°
180°
R
R
R
q variations due to BE
The derivative is around zero in this region, meaning that the sensitivity to external fields is extremely small
j

## Slide 6: "Barber Pole" approach:
Barber pole
A thin metal film of a ferromagnetic conductor is deposited and magnetized along the easy axis
A highly conductive layer (e.g. Al), is deposited on top and patterned in order to form a series of 45 - degrees oriented stripes
The fact that the Al layer is much more conductive than the underlying magnetic one, forces the current to cross the gaps between the Al stripes along the direction of minimum distance, which is perpendicular to the aluminum stripe edges. Then the current density in the ferroelectric materials between the conducting stripes form a 45° angle with permanent magnetization.
BM
J
BM
45°

## Slide 7: Magnetic field sensor based on AMR
Maximum slope
Aluminum
stripes (very low resistivity)
Ferromagnetic
material
(high resistivity)
BE
45°
For BE=0 q=45°
Maximum sensitivity
Variations produced by the external magnetic field HE oriented along the sensitive axis

## Slide 8: Magnetic field sensor based on AMR

## Slide 9: Effect of reversing the permanent magnetization
BM
BE
b
B
J
q
J
3
4
p
The sign of the resistance variation caused by BE is reversed

## Slide 10: Wheatstone bridge of AMR resistors
R1
R1
R4
R4
R2
R3
R2
R3

## Slide 11: Offset free read cycle
The offset is due to mismatch of the zero-field resistors (R0) of the Wheatstone bridge
Phase 1
Phase 2
Inverting the magnetization of all AMR resistors change the sign of the output voltage but leaves the offset unchanged
Phase 1
Phase 2
Offset
phase 1 - phase 2
(no offset)

## Slide 12: Integrated AMR sensor with magnetization coil (set-reset coil)
Iset-reset
order of 1 A for 1ms
Sensitivity axis

## Slide 13: Very sensitive magnetic sensors
Giant Magneto-Resistance (GMR) sensors
Tunnelling Magneto-Resistance (TMR) sensors
Applications.
Hard Disk Head
Solid-State magneto-resistive RAMs (MRAMs)
Detection of magnetically-labelled bio-markers

## Slide 14: Giant Magneto Resistance (GMR) Sensors
Ferro Magnetic (FM) Layers (medium conductivity)
Non-FM, high conductivity layer (e.g. Cu)
Layer thickness:
a few monolayers
R
With no external field, magnetization tends to be opposite in adjacent layers
High surface scattering in the conductive layers.
High resistance
Quantum Mechanics principle:
Spin-dependent scattering

## Slide 15: Effect of an external field
An external field of sufficient strength force all the layers to have parallel magnetization
HE
Low scattering
Low resistance
Resistance variations can be much larger than in AMR sensors (up to 100 %), but this is not a linear effect (it is rather a threshold effect).

## Slide 16: GMR Spin Valve
R
Top view
FM layer with pinned magnetization (does not change with external field)
For null external fields, magnetization
in the two layers are orthogonal
Top FM layer
(the magnetization is affected by
the external field)
HE
R
0
The external field make the two magnetization tend to a parallel or anti-parallel orientation
Linear behavior
around the origin
HE

## Slide 17: TMR (Tunneling Magneto Resistance)
Tunnel current
Free Magnetization Layer
Insulating (tunnel) Layer
Pinned Magnetization Layer
0
HE
The resistance curve is similar to that of GMR, but variations are even larger

## Slide 18: Flux-Gates Magnetometer : Principle
Excitation coil
Sensing coil
VS
H
IM
The fluxgate principle is effective also with soft magnetic materials. What is essential is the presence of saturation.
HIM: the excitation field, proportional to IM
Hext: is the external field, that we want to sense
For Hext=0
IM is a sinusoidal current
In the case of Hext=0, the sensed voltage VS has the property of half-wave symmetry. Then it has no even harmonics

## Slide 19: Flux-Gates Magnetometer : Principle
Excitation coil
Sensing coil
VS
H
IM
The external field Hext, shifts the excitation field H (in the example H is shifted up). As a result, magnetic induction B spends more time in the positive saturation value (BMAX) than in the negative one (.-BMAX).
This introduce an asymmetry that results in the presence of a second harmonic component.
The relationship between the magnitude of the second harmonics and Hext is linear for small values of the field. The sign of Hext is represented by the phase of the second harmonics that can be detected by means of a synchronous demodulator.
For Hext=0